ATLAS

API 579-1 / ASME FFS-1 Part 9

KPTC / RPTC — Help & User Tutorial

Plate with Central Through-Wall Crack | Level 2 FAD | Crack Growth | Remaining Life | Level 3

Software interface concept: crack-case selection, input tabs, results and plots.

Prepared by Dr. Ramana Podugu, M.Tech., MISTE., MIE., MIPE., PhD.

Pythagoras Engineering Services and Consultancy

# How to Use This Help Manual

This document is written as the content source for the Help menu of the ATLAS KPTC/RPTC desktop software. It combines operating instructions, engineering theory, formulas, numerical examples, interpretation of results, troubleshooting guidance and a quick-reference section. A user should be able to open Help, follow the workflow, prepare a case, run the solver and understand the principal outputs without opening the program source code.

Engineering responsibility: The program supports an API 579-1/ASME FFS-1 Part 9 assessment. The final applicability decision, material-property basis, loading definition, remaining-life use, inspection interval and disposition must be reviewed by a qualified engineer.

# Help Contents

| Section | Topic |
| --- | --- |
| 1 | Getting Started and Software Workflow |
| 2 | Theory: KPTC/RPTC and Failure Assessment Diagram |
| 3 | Unit System and Material Database |
| 4 | Crack Geometry and Flaw Characterization |
| 5 | Material Strength and Fracture Toughness |
| 6 | Loads, Secondary Stress and Residual Stress |
| 7 | Level 2 FAD Calculation — Complete SI Numerical Example |
| 8 | Constant-Amplitude Crack-Growth Tutorial |
| 9 | Variable-Amplitude Crack-Growth Tutorial |
| 10 | Remaining Life and Inspection Planning |
| 11 | Level 3 Assessment Features |
| 12 | Results, Dashboard and Plot Interpretation |
| 13 | How to Run the Program |
| 14 | Common Errors and Troubleshooting |
| 15 | Quick Reference Equations and Glossary |
| 16 | Pre-Run and Post-Run Engineering Checklists |

# 1. Getting Started and Software Workflow

## 1.1 What the KPTC/RPTC case does

The KPTC/RPTC case evaluates a plate containing a central through-wall crack. The stress-intensity-factor solution is KPTC (Annex 9B.3.1) and the corresponding reference-stress solution is RPTC (Annex 9C.3.1). The software performs the initial Level 2 FAD assessment, determines the limiting flaw size, calculates fatigue crack growth and remaining life, and can optionally perform Level 3 sensitivity and Method D ductile-tearing studies.

## 1.2 Recommended user workflow

Start a new KPTC/RPTC case and select Constant Amplitude or Variable Amplitude loading.

Select the unit system before entering case-specific values.

Enter crack geometry and flaw characterization.

Select the material record and confirm the strength basis.

Select the fracture-toughness route and verify Kmat.

Select the crack-growth model and verify C, n, threshold and R-ratio treatment.

Enter primary and secondary stresses, then select the residual-stress method.

For variable loading, define the load spectrum.

Set numerical controls, required life, life margin and inspection fraction.

Run the solver, then review Dashboard, FAD, crack-growth history, limiting flaw, remaining life, warnings and plots.

User-interface principle: The desktop application should present these steps as a guided sequence. The user should not need to edit Python files or database CSV files during normal engineering use.

## 1.3 What the user enters and what the program calculates

| User provides | Program calculates |
| --- | --- |
| Unit system, project identity, loading type | Active units, converted database displays and selected-unit outputs |
| t, W, measured crack size and flaw characterization | Assessment crack half-length c0 and applicability ratios |
| Material and strength source | Sy, Su, Lr(max), E, nu |
| Toughness route / project data | Kmat and toughness traceability |
| Primary, secondary and residual stresses | KIP, KISR, reference stress, Lr, Phi, Kr and FAD margin |
| Growth model and load history | Kmin, Kmax, DeltaK, dc/dN, cycle increments and crack-growth history |
| Required life and project factors | Remaining-life acceptance, allowable service life and inspection interval |

# 2. Theory: KPTC/RPTC and Failure Assessment Diagram

## 2.1 Physical problem

The geometry is a finite-width flat plate with a central through-wall crack of total length 2c. The plate thickness is t and the plate half-width is W. The crack is assessed using Mode I opening stress intensity. Primary stresses control both fracture and plastic collapse. Secondary and residual stresses contribute to crack-tip driving force and are treated separately in the FAD interaction procedure.

## 2.2 FAD concept

The Failure Assessment Diagram combines two competing failure mechanisms. The horizontal coordinate Lr measures proximity to plastic collapse through reference stress. The vertical coordinate Kr measures crack-driving force relative to fracture toughness. An assessment point inside or on the applicable FAD is acceptable for that assessed condition; a point outside is unacceptable.

Lr = sigma_ref / Sy

Kr = [KIP + Phi · KISR] / Kmat

For the Level 2 FAD implemented in this case, the allowable curve is:

Kr,allow = (1 - 0.14 Lr^2) [0.3 + 0.7 exp(-0.65 Lr^6)]

## 2.3 Why KIP and KISR are kept separate

Primary loading is required for equilibrium and contributes to both KIP and reference stress. Secondary and residual stresses are not treated as additional primary collapse load. Their contribution is included through KISR and the Phi/xi interaction treatment. This distinction is fundamental to the implemented Level 2 assessment.

## 2.4 Limiting flaw and remaining life

After the initial flaw passes, the program increases crack size and repeats the FAD assessment until the assessment point reaches the FAD boundary or another governing stop is encountered. That crack size is the limiting flaw size. Crack-growth integration from the current inspected flaw to this limiting flaw provides the calculated remaining life.

# 3. Unit System and Material Database

## 3.1 Unit-system selection

| Quantity | SI | FPS |
| --- | --- | --- |
| Length | mm | in |
| Stress / strength | MPa | ksi |
| Stress intensity / toughness | MPa√m | ksi√in |
| Temperature | °C | °F |
| J-integral / J-R data | kJ/m² | program FPS convention |
| Crack-growth rate | mm/cycle | in/cycle |

Select SI or FPS before entering new values. Database displays and default template formulas follow the selected system. Values typed manually are interpreted in the currently selected system. If an already populated case must be converted, use the supplied conversion utility rather than only changing the dropdown.

Existing typed case: Changing the unit dropdown by itself does not mathematically convert previously typed numeric values. Use the conversion utility or re-enter the case values in the new unit system.

## 3.2 Material selection

The material database contains specification, grade/class, product form, condition, material class, specified minimum yield and tensile strengths, typical elastic modulus, exemption-curve assignment, Lr(max) category, default crack-growth model and suggested toughness route. The reference numerical example uses REFERENCE_CS_350 as an ATLAS regression material rather than a real material specification.

| Reference property | Value |
| --- | --- |
| Sy | 350 MPa |
| Su | 500 MPa |
| E | 200,000 MPa |
| nu | 0.30 |
| Kmat | 100 MPa√m |
| Paris C | 2.0E-9 mm/cycle/(MPa√m)^3 |
| Paris n | 3 |
| DeltaK threshold | 5 MPa√m |

## 3.3 Strength source and Lr(max)

The reference case uses DATABASE_SPEC_MIN. If PROJECT_AT_TEMPERATURE is selected, approved project values should be entered. The reference material uses the FLOW_STRESS Lr(max) category:

Lr,max = (Sy + Su) / (2 Sy) = (350 + 500) / (2 × 350) = 1.214286

# 4. Crack Geometry and Flaw Characterization

## 4.1 Reference geometry

| Input | Value | Meaning |
| --- | --- | --- |
| Plate thickness t | 20 mm | Through-thickness dimension |
| Plate half-width W | 400 mm | Centreline to plate edge |
| Measured crack half-length cm | 5 mm | Measured half-length; total crack = 2c |
| Flaw option | OPTION_1 | Use measured crack length directly |

c0 = cm = 5 mm

2c0 = 10 mm

c0/W = 5/400 = 0.0125

The KPTC applicability check requires the crack-to-width ratio to remain within the implemented range. The solver also applies a numerical upper limit to prevent invalid secant behavior as c approaches W.

## 4.2 Option 2 — projected/equivalent crack length

When flaw orientation and biaxial principal stresses require it, Option 2 can be selected. The user supplies the measured crack length, crack angle, principal stresses and projection plane. The workbook calculates the equivalent Mode I assessment half-length before entering the KPTC solution. The shipped reference case uses Option 1, so no projection correction is applied.

# 5. Material Strength, Fracture Toughness and Crack-Growth Data

## 5.1 Fracture toughness

The reference example uses PROJECT_KMAT and therefore takes Kmat = 100 MPa√m directly. The package also contains implemented Annex 9F routes such as project test sets, Section XI lower-bound, Master Curve options, upper-shelf methods, dynamic/arrest adjustments, hydrogen shift, Cr-Mo aging and austenitic-stainless routes. Only the selected route controls the calculation.

Traceability: Always review the Material_Toughness output sheet to confirm the route and source actually used. Do not assume that a database suggestion was automatically selected.

## 5.2 Crack-growth model

The reference case selects FROM_MATERIAL_DB, which resolves to PROJECT_MATERIAL_DATA and a Paris-law form. The basic growth equation is:

dc/dN = C (DeltaK)^n

with a threshold check. For the reference case, C = 2.0E-9 mm/cycle/(MPa√m)^3, n = 3 and DeltaKth = 5 MPa√m.

## 5.3 Effective stress ratio R

The selected R-ratio basis is INCLUDE_RESIDUAL. The residual SIF is therefore included in the effective minimum and maximum crack-tip state used for R-dependent growth-model logic:

R = (Kmin + Kres) / (Kmax + Kres)

Residual stress is not incorrectly cycled from zero; it remains present while the applied loading changes.

# 6. Loads, Secondary Stress and Residual Stress

## 6.1 Reference load input

| Stress component | Value | Role |
| --- | --- | --- |
| Primary membrane Pm | 120 MPa | KIP and reference stress |
| Primary bending Pb | 30 MPa | KIP and reference stress |
| Crack-face pressure pc | 0 MPa | Primary crack opening; may also enter reference stress when enabled |
| Secondary membrane Sm | 20 MPa | KISR and fatigue applied range |
| Secondary bending Sb | 10 MPa | KISR and fatigue applied range |
| Residual membrane Rm | 15 MPa | KISR; fixed through the applied cycle |
| Residual bending Rb | 5 MPa | KISR; fixed through the applied cycle |

## 6.2 Polynomial stress option

Instead of directly entering membrane and bending values, the program can accept fourth-order through-wall polynomial stress coefficients. The membrane and bending components are obtained from the polynomial using the implemented Part 9 transformations:

Pm = P0 + P1/2 + P2/3 + P3/4 + P4/5

Pb = -P1/2 - P2/2 - 9P3/20 - 2P4/5

The same transformation is available for the secondary-stress polynomial. The reference numerical example uses direct membrane+bending input.

## 6.3 Residual-stress methods

The reference example selects USER_DEFINED and uses Rm = 15 MPa and Rb = 5 MPa. The package also provides Annex 9D PWHT uniform, as-welded conservative envelope and uniform-yield routes. Pressure-test residual-stress credit is gated unless it can be quantified for the specific case.

# 7. Level 2 FAD Calculation — Complete SI Numerical Example

## 7.1 Geometry parameter psi

psi = t / (c sqrt(10)) = 20 / (5 sqrt(10)) = 1.26491

## 7.2 Bending correction Mb

Mb = [0.302327 + 70.50193 psi + 110.305 psi^2] / [1 + 110.960 psi + 98.7089 psi^2 + 0.753594 psi^3]

Mb = 0.8841645

## 7.3 Finite-width correction fw

fw = sqrt[sec(pi c / 2W)] = sqrt[sec(pi×5/(2×400))] = 1.00009639

## 7.4 Primary stress-intensity factor

Convert c = 5 mm to 0.005 m for MPa√m units:

sqrt(pi c) = sqrt(pi × 0.005) = 0.125331 sqrt(m)

KIP = fw [(Pm + pc) + Mb Pb] sqrt(pi c)

KIP = 1.00009639 [120 + 0 + 0.8841645×30] × 0.125331 = 18.365947 MPa√m

## 7.5 Secondary + residual stress-intensity factor

KISR = fw [(Sm + Rm) + Mb(Sb + Rb)] sqrt(pi c)

KISR = 1.00009639 [(20+15) + 0.8841645(10+5)] × 0.125331 = 6.049386 MPa√m

## 7.6 RPTC reference stress and Lr

sigma_ref = [Pb + sqrt(Pb^2 + 9Pm^2)] / [3(1 - c/W)]

sigma_ref = [30 + sqrt(30^2 + 9×120^2)] / [3(1 - 5/400)] = 132.066781 MPa

Lr = 132.066781 / 350 = 0.3773337

## 7.7 Secondary-stress interaction

For the plane-strain setting the effective-crack correction is calculated first. For this initial point the program obtains:

| Quantity | Initial value |
| --- | --- |
| Phi0 | 1.0015836 |
| KJ,SR = Phi0 KISR | 6.05897 MPa√m |
| X = Lr(KJ,SR/KIP) | 0.1244832 |
| xi from Table 9.3 interpolation | 1.0558191 |
| Phi = Phi0 xi | 1.0574910 |

## 7.8 Fracture ratio Kr and initial acceptance

Keff = KIP + Phi KISR = 18.365947 + 1.057491×6.049386 = 24.7631 MPa√m

Kr = Keff / Kmat = 24.7631 / 100 = 0.2476312

Kr,allow = 0.9787808

FAD margin = 0.9787808 - 0.2476312 = 0.7311496 > 0  →  PASS

## 7.9 Limiting flaw search

The solver increases c and repeats the complete assessment. A bisection search refines the point where the FAD margin becomes zero. The reference case gives:

| Limiting quantity | Value |
| --- | --- |
| c_lim | 80.408166 mm |
| Total crack length 2c_lim | 160.816332 mm |
| c_lim/W | 0.2010204 |
| Final Lr | 0.4663661 |
| Final Kr | 0.9650267 |
| Final Kr,allow | 0.9650267 |
| Governing stop | FAD boundary |

# 8. Constant-Amplitude Crack-Growth Tutorial

For constant amplitude, the reference load varies from lambda_min = 0 to lambda_max = 1. The fatigue range uses the cyclic applied primary + secondary stresses. Residual stress remains as a fixed crack-tip contribution for the FAD and for the selected R-ratio treatment.

## 8.1 Initial Kmax, Kmin and DeltaK

Applied membrane at full scale = Pm + Sm = 120 + 20 = 140 MPa

Applied bending at full scale = Pb + Sb = 30 + 10 = 40 MPa

Kmax = 21.981060 MPa√m

Kmin = 0 MPa√m

DeltaK = 21.981060 MPa√m

## 8.2 Threshold and Paris growth rate

DeltaK = 21.981060 > DeltaKth = 5 MPa√m  →  fatigue growth active

dc/dN = 2E-9 × (21.981060)^3 = 2.12410E-5 mm/cycle

## 8.3 First numerical increment

Delta c = 0.02 mm

DeltaN = Delta c / (dc/dN) = 0.02 / 2.12410E-5 = 941.6 cycles

c1 = 5.00 + 0.02 = 5.02 mm;   N1 ≈ 941.6 cycles

## 8.4 Recalculation loop

Recalculate psi, Mb and fw at the new crack size.

Calculate Kmax, Kmin and DeltaK.

Apply threshold and evaluate the selected growth equation.

Calculate the cycle increment needed for the numerical crack increment.

Update crack size and cumulative cycles.

Recalculate KIP, KISR, sigma_ref, Lr, Phi, Kr and FAD margin.

Check limiting flaw, c/W limit and maximum-cycle guard.

Repeat until the first governing stop is reached.

## 8.5 Final constant-load result

| Quantity | Reference result |
| --- | --- |
| Current crack half-length | 5 mm |
| Limiting crack half-length | 80.408166 mm |
| Calculated remaining life | 380,411.61 cycles |
| Life acceptance | ACCEPTABLE for the reference controls |
| Governing stop | FAD boundary |

# 9. Variable-Amplitude Crack-Growth Tutorial

## 9.1 Reference load spectrum

| Block | Min scale | Max scale | Cycles | Cycle fraction |
| --- | --- | --- | --- | --- |
| A | 0.00 | 0.70 | 500 | 0.50 |
| B | 0.07 | 0.80 | 300 | 0.30 |
| C | 0.09 | 0.90 | 150 | 0.15 |
| D | 0.10 | 1.00 | 50 | 0.05 |

One complete reference spectrum contains 1,000 cycles. The current package evaluates the growth contribution of the spectrum at each crack size and uses a cycle-weighted equivalent growth rate. It does not currently advance the crack sequentially after each individual block.

Method visibility: The software Help and Results should explicitly state “Equivalent Spectrum / cycle-weighted growth” so the user knows which variable-load algorithm is being applied. A future block-by-block method can be provided as a separate selectable method.

## 9.2 Initial block ranges

At c = 5 mm, the full-scale fatigue Kmax is approximately 21.98106 MPa√m. Each block scales the applied cyclic stresses. The block range is determined from its maximum and minimum scale. Approximate initial values are:

| Block | Kmin (MPa√m) | Kmax (MPa√m) | DeltaK (MPa√m) |
| --- | --- | --- | --- |
| A | 0.0000 | 15.3867 | 15.3867 |
| B | 1.5387 | 17.5848 | 16.0462 |
| C | 1.9783 | 19.7829 | 17.8047 |
| D | 2.1981 | 21.9811 | 19.7830 |

## 9.3 Equivalent spectrum range and growth rate

DeltaK_eq = [sum(w_i DeltaK_i^n)]^(1/n) ≈ 16.25457 MPa√m

(dc/dN)_eq = C (DeltaK_eq)^n ≈ 8.58927E-6 mm/cycle

## 9.4 First variable-load crack increment

DeltaN = 0.02 / 8.58927E-6 ≈ 2328.5 cycles

c1 = 5.02 mm

The program then recalculates every block range at the new crack size, recomputes the equivalent growth rate, advances the crack and performs the maximum-load FAD check. Block D contains the maximum load scale of 1.0 and controls the maximum-load envelope in the reference spectrum.

## 9.5 Final variable-load result

| Quantity | Reference result |
| --- | --- |
| Current crack half-length | 5 mm |
| Limiting crack half-length | 80.408166 mm |
| Calculated remaining life | 940,748.41 cycles |
| Equivalent 1,000-cycle spectra | 940.748 |
| Critical maximum-load block | D |
| Governing stop | FAD boundary |

# 10. Remaining Life and Inspection Planning

The controls sheet distinguishes calculated remaining life from the allowable operating period and inspection interval. This avoids treating the raw crack-growth life as the automatically permitted service interval.

| Control | Reference value |
| --- | --- |
| Current flaw basis | CURRENT_INSPECTED_FLAW |
| Required remaining life | 100,000 cycles |
| In-service life margin factor | 2.0 |
| Minimum calculated life for acceptance | 200,000 cycles |
| Inspection fraction of allowable life | 0.50 |

## 10.1 Acceptance requirement

Minimum calculated life = Required life × Life margin factor

= 100,000 × 2 = 200,000 cycles

Both reference cases exceed 200,000 cycles and therefore pass the selected remaining-life criterion.

## 10.2 Allowable service life

Allowable service life = Calculated remaining life / Life margin factor

| Case | Calculated life | Allowable service life |
| --- | --- | --- |
| Constant | 380,411.61 | 190,205.80 cycles |
| Variable | 940,748.41 | 470,374.20 cycles |

## 10.3 Inspection interval

Inspection interval = Inspection fraction × Allowable service life

| Case | Inspection fraction | Recommended interval |
| --- | --- | --- |
| Constant | 0.50 | 95,102.90 cycles |
| Variable | 0.50 | 235,187.10 cycles |

Project-defined controls: The life margin factor and inspection fraction are project/engineering controls, not universal API 579 constants. The engineer should select them using the governing inspection code, uncertainty, consequence and service conditions.

## 10.4 Optional cycles-to-years conversion

If operating cycles per year are entered, the program can convert remaining life, allowable life and inspection interval into years. The shipped reference case leaves cycles/year blank, so time-based values are not reported.

# 11. Level 3 Assessment Features

## 11.1 Method A sensitivity analysis

When enabled, the package varies selected uncertain inputs one at a time and repeats the complete FAD, limiting-flaw, crack-growth and remaining-life calculation. The default reference sensitivities include primary stress, secondary stress, residual stress, initial flaw size, Kmat, strength, Paris C and DeltaK threshold. A combined adverse case is also evaluated.

| Input varied | Default low | Default high |
| --- | --- | --- |
| Primary stress | -10% | +10% |
| Secondary stress | -20% | +20% |
| Residual stress | -30% | +30% |
| Initial flaw c0 | -20% | +20% |
| Kmat | -20% | +20% |
| Sy and Su | -10% | +10% |
| Paris C | -50% | +100% |
| DeltaKth | -20% | +20% |

For the shipped constant-load case, 2 of 17 sensitivity cases are not acceptable under the selected life criterion. The variable reference case reports all sensitivity cases acceptable. This is a warning about input uncertainty, not a replacement for engineering judgement.

## 11.2 Partial-safety-factor case

The package includes optional project factors on primary stress, toughness and flaw size. The reference workbook has this case disabled. When enabled, the factors are project-defined values and should not be presented as an API-prescribed universal set.

## 11.3 Method D ductile tearing

Method D uses a J-R resistance curve to represent stable ductile tearing. The reference setup uses a Table 9F.3 record and evaluates toughness as tearing extension increases. Each tearing increment is added to the crack, converted to an equivalent K toughness and assessed on the FAD.

J_R = C_R (Delta a)^nR

For the reference record, the package reports no unstable tearing within the assessed range and an instability load factor of about 3.009. The output also carries applicability warnings; J-R data must be appropriate for the actual material, thickness and assessment temperature.

# 12. Results, Dashboard and Plot Interpretation

## 12.1 Output workbook

| Output sheet | What the user should check |
| --- | --- |
| Dashboard | Selected units, initial status, limiting flaw, calculated life, allowable life, inspection interval and warnings |
| Summary | Principal inputs and final outputs |
| FAD | Initial point, growth locus, final governing point and allowable curve |
| Crack_Growth | c, cycles, DeltaK, R and dc/dN history |
| SIF_vs_c | Primary, secondary/residual and fatigue SIF variation with crack length |
| Material_Toughness | Kmat route, source and applicability notes |
| Residual_Stress | Residual method and values/profile used |
| Calculation_Trace | Calculation sequence and API references |
| Part9_Checklist | Coverage and engineering-review items |
| L3_Sensitivity | Uncertainty/sensitivity results |
| L3_Method_D | Ductile-tearing analysis when enabled |

## 12.2 Plot set

| Plot | Interpretation |
| --- | --- |
| P01 crack length vs cycles | Growth history and acceleration toward the limiting flaw |
| P02 K vs cycles | Evolution of crack-driving force |
| P03 dc/dN vs DeltaK | Growth-law response and threshold behavior |
| P04 SIF vs crack length | SIF increase with crack size |
| P05 FAD + growth locus | How the assessment point moves toward the failure boundary |
| P06 Lr/Kr vs crack length | Separate evolution of collapse and fracture ratios |
| P07 FAD margin vs cycles | Remaining assessment margin as the crack grows |
| P08 remaining life / inspection | Calculated life, allowable life and inspection basis |
| P09 load cycle / load blocks | Constant load range or variable spectrum |
| P10 residual stress | Residual stress representation |
| P11 sensitivity tornado | Inputs that most affect life |
| P12 sensitivity FAD cases | Effect of uncertainty on assessment points |
| P13 Method D tearing locus | Stable tearing path on FAD |
| P14 J-R curve / toughness | Resistance curve and toughness evolution |

# 13. How to Run the Program

## 13.1 Desktop software workflow

Create/open a KPTC/RPTC case.

Select units and loading type.

Complete the guided input tabs.

Use Save before running.

Choose Run from the toolbar/menu.

Review the Results tab first, then Plots.

Open Help at any time for field definitions, theory, formulas and troubleshooting.

## 13.2 Python package workflow

The same engine can be run directly from the supplied package. Normal users of the desktop application do not need these commands, but they are useful for validation and engineering support.

| Action | Command |
| --- | --- |
| Run constant case | python RUN_THIS_CASE.py (inside CONSTANT_LOAD) |
| Run variable case | python RUN_THIS_CASE.py (inside VARIABLE_LOAD) |
| Run both cases | python ENGINE/run_case.py (from package root) |
| Write full history CSV + summary JSON | python RUN_THIS_CASE.py --extras |
| Convert an existing typed workbook | python ENGINE/tools/convert_units.py <workbook> --to FPS or --to SI |
| Run validation suite | python ENGINE/validation/test_suite.py |

## 13.3 Output replacement behavior

Each run replaces the previous OUTPUT and PLOTS for that case. If a prior result must be retained for comparison or client records, copy it to a separate project folder before rerunning.

# 14. Common Errors and Troubleshooting

| Symptom | Likely cause / action |
| --- | --- |
| Results appear unreasonable after switching SI/FPS | Typed values were not converted. Use the conversion utility or re-enter values in the selected system. |
| No crack growth | Check DeltaK versus threshold, load scales, selected growth model and units. |
| Immediate FAD failure | Check flaw size, primary load, toughness, residual stress, material strength and units. |
| Material field says project data required | Enter approved project strength/toughness/growth data and set project data status appropriately. |
| Toughness warning | Check temperature, material class, product form and route applicability. |
| Level 3 sensitivity has failing cases | Investigate uncertainty; do not rely only on the base-case PASS. |
| Method D warning | Verify J-R data applicability to actual material, thickness and temperature. |
| Outputs not found | Ensure the case folder and ENGINE folder retain the supplied structure and that the run completed without Python errors. |
| Old results disappeared | This is expected: each run clears and rebuilds OUTPUT/PLOTS for the case. |

# 15. Quick Reference Equations and Glossary

## 15.1 Core equations

psi = t / (c sqrt(10))

Mb = [0.302327 + 70.50193 psi + 110.305 psi^2] / [1 + 110.960 psi + 98.7089 psi^2 + 0.753594 psi^3]

fw = sqrt[sec(pi c / 2W)]

KIP = fw [(Pm + pc) + Mb Pb] sqrt(pi c)

KISR = fw [(Sm + Rm) + Mb(Sb + Rb)] sqrt(pi c)

sigma_ref = [Pb + sqrt(Pb^2 + 9Pm^2)] / [3(1 - c/W)]

Lr = sigma_ref / Sy

Phi = Phi0 xi

Kr = [KIP + Phi KISR] / Kmat

Kr,allow = (1 - 0.14Lr^2)[0.3 + 0.7exp(-0.65Lr^6)]

dc/dN = C(DeltaK)^n

DeltaN = Delta c / (dc/dN)

Nallowable = Nremaining / life margin factor

Ninspection = inspection fraction × Nallowable

## 15.2 Glossary

| Symbol / term | Meaning |
| --- | --- |
| t | Plate thickness |
| W | Plate half-width, centreline to edge |
| c | Current through-wall crack half-length |
| Pm | Primary membrane stress |
| Pb | Primary bending stress |
| pc | Crack-face pressure |
| Sm / Sb | Secondary membrane / bending stress |
| Rm / Rb | Residual membrane / bending stress |
| KIP | Primary Mode I stress intensity factor |
| KISR | Secondary + residual Mode I SIF contribution |
| Sy / Su | Yield / tensile strength used in the assessment |
| Kmat | Fracture toughness used by the FAD |
| sigma_ref | Reference stress for plastic-collapse assessment |
| Lr | Reference-stress ratio |
| Kr | Fracture ratio |
| Phi, xi | Secondary-stress/plasticity interaction terms |
| DeltaK | Fatigue stress-intensity-factor range |
| C, n | Crack-growth-law constants |
| DeltaKth | Threshold stress-intensity-factor range |
| FAD margin | Kr,allow - Kr |
| Limiting flaw | Crack size at first governing assessment limit |
| Remaining life | Calculated cycles from current flaw to limiting condition |

# 16. Pre-Run and Post-Run Engineering Checklists

## 16.1 Pre-run checklist

Correct crack case selected: KPTC/RPTC central through-wall crack.

Correct unit system selected before entering values.

Geometry dimensions and crack measurements verified from inspection/drawing.

Flaw characterization option appropriate.

Material specification, product form, heat treatment and strength source verified.

Toughness route appropriate for material and assessment temperature.

Crack-growth model applicable to material, environment, temperature and R range.

Primary and secondary stresses classified correctly.

Residual-stress method appropriate; project/Annex 9D assumptions recorded.

Constant load range or variable spectrum verified against future service.

Required life, life margin, inspection fraction and cycle rate approved.

Level 3 options enabled only when supporting data are appropriate.

## 16.2 Post-run checklist

Initial FAD status and applicability warnings reviewed.

KIP, KISR, sigma_ref, Lr, Phi and Kr checked for reasonableness.

Limiting crack size is within the intended numerical/applicability domain.

Crack-growth history is monotonic and growth rate behavior is reasonable.

Variable-load method and governing block are understood.

Calculated remaining life exceeds the selected minimum acceptance life.

Allowable service life and inspection interval are understood as project-controlled quantities.

Sensitivity cases reviewed; adverse cases investigated.

Method D results used only with valid J-R data.

Dashboard, Calculation_Trace and Part9_Checklist saved with the engineering record.

Final use: A PASS result from the software should be treated as one part of an engineering Fitness-For-Service decision. Inspection quality, future loading, environment, damage mechanism, uncertainty, monitoring and remediation requirements must also be considered.

# Appendix A. Suggested In-Application Help Topics

For the desktop application Help menu, the manual can be split into the following selectable topics. Each topic can open as a note/article in the Help pane.

| Help topic | Suggested content |
| --- | --- |
| Getting Started | Case selection, units, tabs, save/run/result workflow |
| Crack Geometry | KPTC geometry, c/W, Option 1/2, applicability |
| Material | Database selection, strength source, Lr(max) |
| Fracture Toughness | Kmat methods and applicability |
| Crack Growth | Growth models, threshold, R ratio, constant vs variable |
| Loads | Primary/secondary classification and polynomial option |
| Residual Stress | User-defined and Annex 9D routes |
| FAD Theory | KIP, KISR, sigma_ref, Lr, Phi/xi, Kr and acceptance |
| Remaining Life | Limiting flaw, life margin, allowable life, inspection interval |
| Level 3 | Sensitivity, PSF and Method D |
| Results | Dashboard and output workbook |
| Plots | Meaning of each plot |
| Troubleshooting | Common unit/data/run problems |
| Equations | Quick equation reference |
| Worked Example | Complete SI numerical example |

# Appendix B. Suggested Help Integration in the Desktop Tool

The existing menu already includes Help. A practical implementation is to expose the manual as searchable topics rather than one long page. Recommended structure:

Help > Getting Started

Help > Input Tabs

Help > KPTC/RPTC Theory

Help > Worked SI Example

Help > Constant Crack Growth

Help > Variable Load Growth

Help > Remaining Life

Help > Level 3

Help > Results and Plots

Help > Troubleshooting

Help > About / Version / API 579 edition

Context-sensitive Help can later be added so pressing F1 or clicking a help icon beside a field opens the relevant topic, for example Kmat, Lr(max), residual stress, DeltaK threshold or inspection fraction.